Recipes for Making Pigments:

These recipes were based on instructions found at Pigments Through the Ages (http://www.webexhibits.org/pigments/) and from trial and error in my chemistry classes.

Cobalt Blue:

Take 2.0 g of Cobalt chloride hexahydrate (CoCl2 • 6H2O) and grind it with 10.0 g of Aluminum chloride (Al2Cl3) in a mortar. Heat the mixture in a test tube for 3-4 minutes. This recipe might produce a pinkish solution that dries to a bright cyan blue. This is a characteristic of cobalt chloride – it is pink when hydrated and blue when dry.

Prussian Blue:

4.0 g of Ferric chloride (FeCl3) in 100 mL of dionized water is slowly poured into a stirred solution of 2.0 of Potassium hexacyanoferrite (K4[F3(CN)6]) in 100 mL of water. Stir while pouring through filter paper. Place in an evaporation dish or flask and dry at 100 °C on a hot plate.

Cobalt Violet:

4.0 g of Cobalt chloride hexahydrate (CoCl2 • 6H2O) and 2.6 g of sodium hydrogen phosphate (NaH2PO4 • 10H2O) each dissolved in 20 mL of water. Then pour together, filter, and dry.

Yellow Ochre:

2.0 of Cobalt chloride hexahydrate (CoCl2 • 6H2O). Acidify it with 2 mL of glacial acetic acid. Slowly mix in 16.0 g of Potassium nitrite (KNO2). Add water and gum Arabic.

Lemon Yellow:

Add 2.0 g of Barium Chloride to 20 mL water in a small beaker. Add 2.0 g of Potassium Chromate to 20 mL water in another beaker. Dissolve both. Then mix both beakers together.

Carmine:

5.0 g powdered cochineal is boiled in 350 mL of distilled water until the volume has been slowly reduced to about 150 mL; add 7.5 mL of dilute ammonia solution, then filter and bottle. Ammonia can be replaced with alum or vinegar or cream of tartar to produce different shades. To make a lake, some of the pigment is added to 5 g of ground natural chalk which has been washed and filtered.

India Black (Carbon Black):

Take a charcoal briquette and grind it up to a fine powder in a mortar and pestle, or use soot. Strain through a sieve to remove any larger grains. Add distilled water to make a paste and a few drops of vinegar.

Verdegris (Grecian Green):

Take sheets of thick gauge (22 gauge) unvarnished copper sheeting and clean them with dish soap, making sure to handle them only by the edges. Make a solution of vinegar and salt, then dip paper towels into it and stack the copper sheets with alternating layers of the soaked paper towels. Place in a sealed plastic container (such as a sour cream tub)  and allow to sit for several days. Green copper (II) acetate will form, which can be scraped off with a knife and used for pigment.

Adding Binder:

To all recipes, add 2 mL of Gum Arabic as a binder. A few drops of rubbing alcohol can be used as a dispersant to spread pigment grains around. Place your final pigment in a small vial and label it with the name of the pigment and the date.

Try experimenting with these recipes, and you may get a better result. Some of the formulas work consistently, others will require some tinkering.

Let me know how these turn out.

David Black

Walden School of Liberal Arts

elementsunearthed@gmail.com